## Slide 1: Evolving API Standards Impact on Engine Lubrication
Cody Evans, CLS
ExxonMobil - Fuels Lubricants & Specialty Marketing

## Slide 2: Agenda
Evolving API Standards
CI-4, CJ-4, CK-4
FA-4
Impact on Engine Lubrication
NOx
HTHS
Oil Drains

## Slide 3: Evolving API Standards

## Slide 4: What are the Drivers of Evolving API Standards?
These drivers played a key role in the development of previous PC-10 specification, which led to CJ-4.
But, now the focus has shifted to reducing CO2 emissions.
Historically, the main drivers to change the industry standards of Heavy Duty Engine Oils have been a call to reduce:
Particulate matter
NOx emissions
Notes: *ULSD – Ultra Low Sulfur content in Diesel

## Slide 5: Industry standards are more demanding than ever before
News standards are calling for vehicle and engine improvements capable of:
Enhancing fuel efficiency
Helping fleets meet their aggressive sustainability-related goals
Further reducing CO2 and greenhouse gas emissions
Chart: COV Class 8 High Roof Fuel Consumption Standards
| 2021 | 2024 | 2027
gallons of fuel per 1,000 Ton-Mile | 7.6 | 6.9 | 6.6

## Slide 6: What is PC-11?
New heavy duty diesel engine oil category from American Petroleum Institute’s (API) set to go into effect December 1, 2016
PC-11 compliant oils will have to pass stringent tests and are designed to provide higher performance than today’s CJ-4 oils

## Slide 7: Advancements in engine technology
Higher engine temperatures
Allow for better combustion in the cylinder and less after treatment (EGR in particular)
Tighter tolerances
Allow for increased fuel efficiency
Notes: “The industry is moving to Higher engine temperatures. The higher temps allow for better combustion in the cylinder and less after treatment (EGR in particular). The down side to the higher engine temperatures is that it puts significant oxidative stress on the oil. (hence why PC-11 oil must have higher oxidation stability).
Higher tolerances in injectors?

## Slide 8: How Can Fuel Efficient Lubricants Impact Fuel Economy?
Fuel
  Fuel is a leading operating cost
  Only 35% of the fuel is used to move the truck
  The rest is lost as heat and friction
Two types of friction
  Viscous friction—Related to the thickness of the oil and includes energy losses related to pumping the oil through the engine
  Contact friction—Results from contact between metal surfaces; can lead to both engine wear and a reduction in fuel economy
Heat: approx. 50%
Friction: 15%
Truck Movement: 35%
Notes: “The industry is moving to Higher engine temperatures. The higher temps allow for better combustion in the cylinder and less after treatment (EGR in particular). The down side to the higher engine temperatures is that it puts significant oxidative stress on the oil. (hence why PC-11 oil must have higher oxidation stability).
Higher tolerances in injectors?

## Slide 9
Energy Efficiency Study

## Slide 10: Current Factory Fill Oil

## Slide 11: Comparing PC-11 oils with today’s CJ-4 oils

## Slide 12: Performance benefits of PC-11 oils compared with CJ-4 oils
Superior Oxidation Stability
Enhanced Shear Stability
Improved Oil Aeration
Better engine performance and durability
Notes: Compare against CJ-4

## Slide 13
Notes: “The industry is moving to Higher engine temperatures. The higher temps allow for better combustion in the cylinder and less after treatment (EGR in particular). The down side to the higher engine temperatures is that it puts significant oxidative stress on the oil. (hence why PC-11 oil must have higher oxidation stability).
Higher tolerances in injectors?

## Slide 14: Oxidative stability benefits
Oxidation is the reaction of oil molecules with oxygen
New PC-11 oils will have to meet the requirements of the stringent Volvo T-13 oxidation test
Oxidation rates increase as engine and oil temperatures increase
Oxidation causes an oil to degrade, shortening its useful life
    Increased viscosity
    Acidic by-products
    Sludge/varnish formation
    Corrosive wear

## Slide 15: Volvo T-13 oxidation test
The definitive performance test for PC-11, jointly developed by Volvo and ExxonMobil
Chart: Test Hours
| 0 | 48 | 96 | 120 | 144 | 168 | 192 | 216 | 240 | 252 | 264 | 276 | 288 | 300 | 312 | 324 | 336 | 348 | 360
DEO-ULS 10W-30 | 0 | -0.017496 | 0.020499 | 0.029899 | 0.035383 | 0.022457 | 0.049615 | 0.23136 | 0.478 | 0.59943 | 0.77699 | 0.9389 | 1.1896 | 1.4168 | 1.7745 | 2.1479 | 2.6859 | 3.2956 | 4.2709
Elite 10W-30 | 0 | -0.021587 | 0.024615 | 0.048045 | 0.052916 | 0.064631 | 0.06621 | 0.065947 | 0.13163 | 0.19179 | 0.2809 | 0.35317 | 0.46637 | 0.5493 | 0.68882 | 0.79545 | 1.0008 | 1.1469 | 1.3878
PC-11B 10W-30 | 0 | -0.027961 | 0.0082237 | 0.03125 | 0.050987 | 0.067434 | 0.080592 | 0.10033 | 0.10526 | 0.11842 | 0.12993 | 0.11842 | 0.12993 | 0.13487 | 0.13487 | 0.15132 | 0.18421 | 0.16776 | 0.28289
Volvo T-13 test criteria:
Peak IR oxidation level (360 hours)
Viscosity increase (final 60 hours)
Designed to age oil to ~50,000+ miles in 360 hours
Turbocharged 500 horsepower, Volvo eight cylinder engine equipped with EGR and running on ULSD. 1,500 RPM for 360 hours, at 130C (266F).

## Slide 16: Shear stability benefits
The shearing of polymers used in multigrade oils into smaller pieces can permanently reduce oil viscosity
  Reduced viscosity can leave critical engine parts vulnerable to serious wear
  Shearing can occur as the oil circulates through an engine and encounters gears, roller followers, piston rings, etc.
  In the past, soot thickening could compensate for shearing, but modern emission-controlled engines produce relatively little soot
CK-4 and FA-4 oils are more shear stable versus today’s CJ-4 oils

## Slide 17: Reduced aeration benefits
Aeration is the introduction of tiny air bubbles into the oil
Aerated oil has diminished ability to cool and lubricate the engine
Aerated oil is more common in today’s emission-controlled engines due to higher operating temperatures and pressures
The Caterpillar Oil Aeration Test (COAT) measures an oil’s ability to release air trapped in the oil
The quicker the oil can release the air, the better
Less air in the oil will result in better lubrication and oxidative stability

## Slide 19: PC-11 is more than just one category change

## Slide 20: PC-11 will have two sub-categories
Enhanced replacement for CJ-4 oils. Fully backwards compatible, and with traditional HTHS* viscosity
CK-4
Improved fuel economy, and lower HTHS* viscosity
*High temperature/high shear
FA-4

## Slide 21: Comparing CK-4 vs. FA-4 oils
While both new categories of PC-11 oils will deliver enhanced benefits over today’s CJ-4 oils, there are fundamental differences between the two categories, as noted below:
CK-4
FA-4
- Backwards compatible to all engines operating on API CJ-4 oils today
- Direct replacement for current API CJ-4 oils
- Traditional HTHS viscosity of 3.5 cP @ 150C minimum
- Available in multiple viscosity grades - XXW-40, XXW-30
- Backwards compatibility not guaranteed – engine make/model specific
- Preferred for some 2017 model engines for enhanced fuel economy
- Lower HTHS viscosity between 2.9 and 3.2 cP @ 150C
- Only available in XXW-30 viscosity grade

## Slide 22: Understanding HTHS and its impact on fuel economy

## Slide 23: What do you mean by High Temperature/High Sheer (HTHS)?
HTHS is the thin film viscosity measurement at high temperature and high sliding speeds such as those encountered in:
Oil pumps
Gearboxes
Shear Rate
Apparent
Viscosity
Base Oil Viscosity
Multigrade Additive - Polymer Contribution
The viscosity contribution of multigrade additive is minimized due to the high shear force
Resulting HTHS viscosity measurement is primarily that of the base oil component alone
Valve trains
Piston rings
Piston liner interfaces

## Slide 24: White Board Discussion
Level 1 – Multi-Viscosity Oil
Level 2 – Base Stock vs VI Improver
Level 3 – 5W-30 vs 10W-30
Level 4 – Low Temp and HTHS
Ilistrations are for general reference only and do not represent all oils in the in the API viscosity categories

## Slide 25
Level 1

## Slide 26
Level 1

## Slide 27
Level 1

## Slide 28
Level 1

## Slide 29
Level 1

## Slide 30
Level 1

## Slide 31
Level 2

## Slide 32
Level 2

## Slide 33
Level 2

## Slide 34
Level 2

## Slide 35
Level 3

## Slide 36
Level 3

## Slide 37
Level 3

## Slide 38
Level 3

## Slide 39
Level 3

## Slide 40
Level 4

## Slide 41
Level 4

## Slide 42
Level 4

## Slide 43
Level 4

## Slide 44
Level 4

## Slide 45
Level 4

## Slide 46
Level 4

## Slide 47
Level 4

## Slide 48: FA-4 oils will have lower HTHS limit, which can help improve fuel economy potential
SAE 20
SAE 30
SAE 40/50
Today’s API CJ-4 15W-40 oils are the baseline for comparison.
Notes: Update chart per Thomas email

## Slide 49: Lower HTHS limits of FA-4 oils can help improve fuel economy potential over today’s CJ-4 oils
SAE 20
SAE 30
SAE 40/50
The new API FA-4 10W-30 oils could provide an approximate 1% improvement in fuel economy vs. today’s 15W-40 baseline

## Slide 50: The difference in 10W-30 formulations
10W-30
10W-30
CK-4
FA-4
Better fuel economy
15W-40
CK-4
Both CK-4 and FA-4 categories will have 10W-30 formulations
But lower high temperature/high shear FA-4 10W-30 oils will provide greater fuel economy potential than CK-4 10W-30s

## Slide 51: Drain Limitations

## Slide 52: Summary

## Slide 53: Summary
Launch date – Dec 1, 2016
CK-4 is an improvement to CJ-4
    Oxidation
    Aeration
    Sheer stability
    Backwards compatible
  FA-4 is chosen by the OEM
    Not backwards compatible
    Even better fuel economy
Action Items
  Follow OEM Recommendations
  Consider Consolidation with Manufacturer Support

## Slide 54: Thank you

## Slide 55: Backup - Ford
Ford has tested low phosphorus (800ppm) CK-4 oil that produced wear in the valve train of their 6.7L Super Duty diesel engine
Ford did not experience this issue with CJ-4 oils (with minimal actual data)
This problem is unique to Ford; no other OEM’s have had similar issues with CK-4 oils
Ford’s new specification, WSS-M2C171-F1, will require passing their valve train wear test for oil qualification
  This test does not exist today and the passing parameters are unknown
  This test will not be available until 2Q17 at the earliest
In the meantime, Ford will allow existing CJ-4 oils (not claiming CK-4) to be used in Ford engines without WSS-M2C171-F1 on the label.
CK-4 oils, based on formulations licensed for CJ-4 before January 2016, with greater than 1000 ppm phosphorus, can gain the approval without needing to pass the valve train wear test until the test is available